## Slide 1
THE COPPER LEACHING FROM ELECTROPLATING WASTE SLUDGE WITH ACIDIC REAGENT
Carlos da Silva BENTO*, Gediz UĞUZ
Ondokuz Mayis University, Chemical Engineering Department
*carlossb@gmail.com
Abstract
The copper leaching from electroplating waste sludge by acidic reagent H2SO4 (sulfuric acid) solution has been studied. In this study electroplating waste sludge was called EWS (acronym for Electroplating Waste Sludge). Characterization of the EWS was performed by using XRD, SEM and F-TIR analysis. The main important leaching parameters are determined as leaching time, particle size, mixing speed, H2SO4 concentration, solid/liquid ratio, and temperature in copper leaching with H2SO4 from EWS. The leaching method has been employed using leaching times ranged from 0 to 420 minutes; particle size ranged from 45-63 µm to 325-230 µm; mixing speed ranged from 400 rpm to 800 rpm; H2SO4 concentrations in solution ranged from 1.2 to 2 M H2SO4; solid/liquid ratioranged from 12:1 mg.mL-1 to 28:1 mg.mL-1 and temperature ranged from 80 oC to 120 oC. Optimum leaching conditions from EWS by H2SO4 are found as leaching times: 120 min; particle size: 45-63 µm; mixing speed: 800 rpm; H2SO4 concentration: 2 M H2SO4; solid/liquid ratio: 12:1 mg.mL-1; temperature: 120 oC. Efficiency of copper leaching was found as 88.10 % with increasing leaching time, particle size, mixing speed, H2SO4 concentration and temperature, with decreasing solid/liquid ratio.
Keywords: Leaching, Copper, H2SO4, Leaching parameters, Electroplating Waste sludge (EWS).
1.Introduction
Around us, there are many objects made of different materials. These different objects are plated to provide chemical and mechanical resistance, desired properties and beauties and to protect against corrosion. Metal plating is one of the most commonly used methods for plating objects. The method based on the principle of depositing metals on the surface in the presence of electric fields is known electroplating [1,2]. Electroplating which is a branch of the metal industry is a method to restorate metal surfaces with chemical and electrochemical processes. This galvanizing process consists of pre-treatment and coating bath. These processes lead to the formation of various types of waste water containing metal such as copper, zinc, iron [3,4]. Aluminum (Al), cadmium (Cd), chromium (Cr), copper (Cu), lead (Pb), nickel (Ni), zinc (Zn) metals and arsenic (As) and boron (B) metalloids are called heavy metals and they have specific gravity greater than five [5].
2. Materıals and Methods
  2.1.Materials and Characterization
EWS that contains heavy metals was used for leaching experiments. Spectrometer Blue model ICP – OES was used for heavy metal analysis of EWS which contains copper, zinc, magnesium, aluminum, lead, tin copper oxide and JEOL JSM-7001F model SEM was used to view morphology of EWS before leaching process for characterization of EWS. For The heavy metal analysis of the EWS is represented in Table 1. Before leaching process, SEM images and FTIR analyses of EWS showed in respectively Figure 1 and Figure 2. Explanation of the FT-IR spectra of EWS is represented in Table 2.
Table 1. The heavy metal analysis of the EWS
Figure 1. SEM images of EWS sludge before leaching process.
Table 2. Explanation of the FT-IR spectra of EWS.
2.2. Sample preparation
The effects of time, particle size, mixing speed, solid/liquid ratio, H2SO4 concentration and temperature were investigated in this study. The heavy metal waste sludge was dried 24 hours in oven at 200 oC for removing water from the EWS. After this processes, it was sieved to get appropriate particle size for experiments.
Figure 3. Graphical abstract of methodology.
2.3. Method
In this study, mixing leaching method was used for leaching experiments. A glass beaker (1000 mL) was used like leaching reactor. A mechanical mixer and a heater respectively were used to obtain desired mixing speed and temperature. The temperature of the leach solution in the reactor was provided by a heater. HANNA HI 8341 pH-meter was used for controlling pH in the leaching solutions before and after leaching experiments. Required amount of EWS desired particle
Figure.4. Diagram of the EWS leaching phenomen
3. Conclusions
EWS was studied by chemical leaching with sulphuric acid. Experimental data showed that operational conditions were very important for leaching processes. Maximum leaching yield (88.10% of Cu) was achieved at pH 2,5 , temperature 120 °C, particle size 45-63 µm sulphuric acid concentration 2M H2SO4, 12:1 (12 g EWS / 1 L H2SO4), and mixing speed 800 rpm. Leaching experiments dates were taken from 0 minute to 420 minutes (60 minutes ranges). These results indicated that the chemical leaching with sulphuric acid is effective for EWS to recover copper. Chemical leaching needs shorter process time than the other leaching techniques. These results suggest that chemical leaching for metal plating waste sludge may be an alternative recovery technique for heavy metals such as copper.
Acknowledgement
We are thankful for Prof. Dr. Feza GEYİKCİ, Prof. Dr. Yıldıray TOPCU and Res. Asst. Rukan Can SEYFELİ for experimental supports and Ondokuz Mayıs University Department of Chemical Engineering for their laboratory facilities.
REFERENCES
[1] S.S. Hosseinia, E. Bringas, N.R. Tan, I.Ortiz, M. Ghahramani, M.A.A. Shahmirzadi, “Recent progress in development of high performance polymeric membranes and materials for metal plating wastewater treatment: A review,”Journal of Water Process Engineering., vol. 9, pp.78–110, 2016.
[2] J. Tan, M. Lee, “NEWater—An Alternative Source of Water for the Wafer FabIndustry In singapore,” Proceeding of Recycling and Alternate Sources for theWafer/PCB Industries Conference, 2001, pp. 11–12.
[3] F.V. Hackbarth, D. Maass, A.A.U. Souza, V.J.P. Vilar, S.M.A.G.U. Souza, “Removal of hexavalent chromium from electroplating wastewaters using marine macroalga Pelvetia canaliculata as natural electron donor,” Chemical Engineering Journal, vol. 290, pp. 477–489, 2016.
[4] M.B. Mansur, S.D.F. Rocha, F.S. Magalhães, J.d.S. Benedetto, “Selective extraction of zinc(II) over iron(II) from spent hydrochloric acid pickling effluents by liquid–liquid extraction, ” J. Hazard. Mater., vol. 150, pp. 669–678, 2008
[5] G. Mustafa, S. Komatsu, “Toxicity of heavy metals and metal-containing nanoparticles on plants,” Biochimica et Biophysica Acta, vol.1864, pp. 932–944, 2016.
Component (%) |  |  |  |  | 
Cu | Zn | Mg | Al | Sn | Pb
10.448 | 2.513 | 1.022 | 0.212 | 0.051 | 0.001
Figure 2. FTIR analysis of EWS sludge before leaching process.
Wavelengt cm-1 | Explanation
3349.98 | EWS has a peak due to the water absorption that vibrates H-O-H.
1633.82 | This peak is due to the water adsorption that vibrates OH bending.
1409.08 | The band at around this wavelength is due to CaO in EWS.
996.83 | The peak is related to fused silica.
871.98 | The band occurs from the translational vibration of OH in EWS.